## Slide 1: Advanced Nanotechnology (Nanoscience)
Properties of
Optical
Electrical
Thermal
Magnetic
Top-down
Bottom-up
Nanomaterials and structures

## Slide 2: Magnetism to Spintronics
Introduction to Solid State Physics
Kittel 8th ed
Chap. 11-13,
Solid State Physics
Ashcroft and Mermin
Chap. 31-33,
Condensed Matter Physics
Marder 2nd ed
Chap. 24-26,
Dr. Shang-Fan Lee
Institute of Physics, Academia Sinica

## Slide 3: Why do most broken permanent magnets repel each other?

## Slide 4: Cooperative phenomena
Elementary excitations in solids describe the response of a solid to a perturbation
  Quasiparticles
  usually fermions, resemble the particles that make the system, e.g. quasi-electrons
  Collective excitations
  usually bosons, describe collective motions
  use second quantization with Fermi-Dirac or Bose- Einstein statistics

## Slide 5: Magnetism
the Bohr–van Leeuwen theorem
when statistical mechanics and classical mechanics are applied consistently, the thermal average of the magnetization is always zero.
Magnetism in solids is solely a quantum mechanical effect
Origin of the magnetic moment:
  Electron spin
  Electron orbital momentum
From (macroscopic) response to external magnetic field
  Diamagnetism  < 0, , insensitive to temperature
  Paramagnetism  > 0, Curie law
  Curie-Weiss law
  Ferromagnetism exchange interaction (quantum)

## Slide 6: Magnetism
巨觀： 順磁性 逆磁性
Paramagnetism diamagnetism
微觀： 鐵磁性 反鐵磁性 亞鐵磁性
Ferromagnetism Antiferromagnetism Ferrimagnetism

## Slide 7: Family Tree of Magnetism

## Slide 8: Why do most broken permanent magnets repel each other?
N
N
N
N
S
S
S
S
?

## Slide 9
Classical and quantum theory for diamagnetism
  Calculate
Classical and quantum theory for paramagnetism
  Superparamagnetism, Langevin function
  Hund’s rules
  Magnetic state
  Crystal field
  Quenching of orbital angular momentum Lz
    Angular momentum operator
    Spherical harmonics
  Jahn-Teller effect
  Paramagnetic susceptibility of conduction electrons

## Slide 10
Ferromagnetism
  Microscopic – ferro, antiferro, ferri magnetism
  Exchange interaction
  Exchange splitting – source of magnetization
  two-electron system spin-independent Schrodinger equation
  Type of exchange: direct exchange, super exchange, indirect exchange, itinerant exchange
  Spin Hamiltonian and Heisenberg model
  Molecular-field (mean-field) approximation

## Slide 11: Ferromagnetic elements: 鐵 Fe, 鈷 Co, 鎳 Ni, 釓 Gd, 鏑 Dy, 錳 Mn, 鈀 Pd ?? Elements with ferromagnetic properties 合金, alloys 錳氧化物 MnOx, ……
Notes: spin ferromagnet 指南車

## Slide 12
Tetrahedron | Cube hexahedron | Octahedron | Dodecahedron | Icosahedron
Platonic solid From Wikipedia
In geometry, a Platonic solid is a convex polyhedron that is regular, in the sense of a regular polygon. Specifically, the faces of a Platonic solid are congruent regular polygons, with the same number of faces meeting at each vertex; thus, all its edges are congruent, as are its vertices and angles.
There are precisely five Platonic solids (shown below):
The name of each figure is derived from its number of faces: respectively 4, 6, 8, 12, and 20.
The aesthetic beauty and symmetry of the Platonic solids have made them a favorite subject of geometers for thousands of years. They are named for the ancient Greek philosopher Plato who theorized that the classical elements were constructed from the regular solids.

## Slide 13
Solar system
s, p electron orbits
Orbital viewer
Electronic orbit

## Slide 14: Resonance
One-dimensional
Two-dimensional
Hydrogen atom
Three-dimensional

## Slide 15
s, p electron orbital
Orbital viewer
3d transition metals:
Mn atom has 5 d  electrons Bulk Mn is NOT magnetic
Co atom has 5 d electrons and 2 d  electrons
Bulk Co is magnetic.
3d electron distribution in real space

## Slide 16
d orbitals
Crystal-field splitting

## Slide 17: Stern-Gerlach Experiment
There are two kinds of electrons: spin-up and spin-down.
Stern and Gerlach: How a Bad Cigar Helped Reorient Atomic Physics
Physics Today 56, 53 (2003) 10.1063/1.1650229

## Slide 18
Stoner criterion for ferromagnetism:
For the non-magnetic state there are identical density of states for the two spins.
For a ferromagnetic state, N↑ > N↓. The polarization is indicated by the thick blue arrow.
I N(EF) > 1, I is the Stoner exchange parameter and N(EF) is the density of states at the Fermi energy.
Schematic plot for the energy band structure of 3d transition metals.
Teodorescu and Lungu, "Band ferromagnetism in systems of variable dimensionality". J Optoelectronics and Adv. Mat. 10, 3058–3068 (2008).

## Slide 19
Stoner band ferromagnetism Teodorescu, C. M.; Lungu, G. A. (November 2008). "Band ferromagnetism in systems of variable dimensionality". Journal of Optoelectronics and Advanced Materials 10 (11): 3058–3068.

## Slide 20
Exchange interaction

## Slide 21
Super exchange interaction
Double exchange interaction
In superexchange, a ferromagnetic or antiferromagnetic alignment occurs between two atoms with the same valence (number of electrons) or differs by two, and the electrons are localized;
while in double-exchange, the interaction occurs only when one atom has an extra electron compared to the other, the electrons are itinerant (delocalized); this results in the material displaying magnetic exchange coupling, as well as metallic conductivity.

## Slide 22
Berry Phase
Aharonov-Bohm Effect
Electrons traveling around a flux tube suffer a phase change and can interfere with themselves even if they only travel through regions where B = 0.
(B) An open flux tube is not experimentally realizable, but a small toroidal magnet with no flux leakage can be constructed instead.
Electron hologram showing interference fringes of electrons passing through small toroidal magnet. The magnetic flux passing through the torus is quantized so as to produce an integer multiple of  phase change in the electron wave functions. The electron is completely screened from the magnetic induction in the magnet. In (A) the phase change is 0, while in (B) the phase change is . [Source: Tonomura (1993), p. 67.]

## Slide 23
Parallel transport of a vector along a closed path on the sphere S2 leads to a geometric phase between initial and final state.
Real-space Berry phases: Skyrmion soccer (invited)
Karin Everschor-Sitte and Matthias Sitte
Journal of Applied Physics 115, 172602 (2014); doi: 10.1063/1.4870695

## Slide 24
Parameter dependent system:
Berry phase formalism for
intrinsic Hall effects
Berry phase
[Berry, Proc. Roy. Soc. London A 392, 451 (1984)]
Adiabatic theorem:
Geometric phase:
From Prof. Guo Guang-Yu

## Slide 25
From Prof. Guo Guang-Yu
Well defined for a closed path
Stokes theorem
Berry Curvature

## Slide 26
From Prof. Guo Guang-Yu
Vector potential
Analogies
Berry curvature
Geometric phase
Berry connection
Chern number
Dirac monopole
Aharonov-Bohm phase
Magnetic field

## Slide 27
From Prof. Guo Guang-Yu
Semiclassical dynamics of Bloch electrons
Old version [e.g., Aschroft, Mermin, 1976]
New version [Marder, 2000]
Berry phase correction [Chang & Niu, PRL (1995), PRB (1996)]
(Berry curvature)

## Slide 28: Demagnetization factor D
can be solved analytically in some cases, numerically in others
For an ellipsoid Dx + Dy + Dz = 1 (SI units) Dx + Dy + Dz = 4 (cgs units)
Solution for Spheroid a = b  c
Prolate spheroid (football shape) c/a = r > 1 ; a = b , In cgs units
Limiting case r >> 1 ( long rod )
Oblate Spheroid (pancake shape) c/a = r < 1 ; a = b
Limiting case r >> 1 ( flat disk)
c
a
a
Note: you measure 2M
without knowing the sample
Note: you measure 4M
without knowing the sample

## Slide 29: Surface anisotropy
:
:
:
For hcp Co For bcc Fe : directional cosines
Surface anisotropy 

## Slide 30: Stoner–Wohlfarth model
A widely used model for the magnetization of single-domain ferromagnets. It is a simple example of magnetic hysteresis and is useful for modeling small magnetic particles
where Ku is the uniaxial anisotropy parameter, V is the volume of the magnet, Ms is the saturation magnetization.

## Slide 31: Ferromagnetic domains
For a 180 Bloch wall rotated in N+1 atomic planes
Wall energy density
: lattice constant
,
in Fe
1 erg/cm2 in Fe
Wall width
Exchange stiffness constant
,
  competition between exchange, anisotropy, and magnetic energies.
  Bloch wall: rotation out of the plane of the two spins
  Neel wall: rotation within the plane of the two spins

## Slide 32
Domain wall energy  versus thickness D of Ni80Fe20 thin films
N < B ~ 50nm
Thick films have Bloch walls Thin films have Neel walls
Cross-tie walls show up in between.
A=10-6 erg/cm
K=1500 erg/cm3
D
D  50nm
Cross-tie zone
N
B
N < B
Further reference: Antonio DeSimone, Hans Knupfer, and Felix Otto, Calculus of Variations 27, 233–253 (2006) 2-d stability of the Neel wall

## Slide 33: Magnetic Resonance
Nuclear Magnetic Resonance (NMR)
  Line width
  Hyperfine Splitting, Knight Shift
  Nuclear Quadrupole Resonance (NQR)
Ferromagnetic Resonance (FMR)
  Shape Effect
  Spin Wave resonance (SWR)
Antiferromagnetic Resonance (AFMR)
Electron Paramagnetic Resonance (EPR or ESR)
  Exchange narrowing
  Zero-field Splitting
Maser
What we can learn:
From absorption fine structure  electronic structure of single defects
From changes in linewidth  relative motion of the spin to the surroundings
From resonance frequency  internal magnetic field
Collective spin excitations

## Slide 34: FMR
Shape effect:
internal magnetic field
=
Equation of motion of a magnetic moment in an external field
To first order
Uniform mode
Landau-Lifshitz-Gilbert (LLG) equation

## Slide 35: Sphere flat plate with perpendicular field flat plate with in-plane field
B0
B0
Uniform mode
Spin wave resonance; Magnons
We can derive
When ka << 1
flat plate with perpendicular field
Consider a one-dimensional spin chain with only nearest-neighbor interactions.
Quantization of (uniform mode) spin waves, then consider the thermal excitation of Mannons, leads to Bloch T3/2 law.

## Slide 36: AFMR
Spin wave resonance; Antiferromagnetic Magnons
We can derive
When ka << 1
Consider a one-dimensional antiferromangetic spin chain with only nearest-neighbor interactions. Treat sublattice A with up spin S and sublattice B with down spin –S, J<0.
AFMR
exchange plus anisotropy fields on the two sublattices
Uniform mode
on M1
on M2

## Slide 37: Spintronics Electronics with electron spin as an extra degree of freedom Generate, inject, process, and detect spin currents
Generation: ferromagnetic materials, spin Hall effect, spin pumping effect etc.
Injection: interfaces, heterogeneous structures, tunnel junctions
Process: spin transfer torque
Detection: Giant Magnetoresistance, Tunneling MR
Historically, from magnetic coupling to transport phenomena
important materials: CoFe, CoFeB, Cu, Ru, IrMn, PtMn, MgO, Al2O3, Pt, Ta

## Slide 38
Spin Transfer Torque
Transverse component
S
Slonczewski JMMM 159, L1 (1996)
The transverse spin component is lost by the conduction electrons, transferred to the global spin of the layer
S
Experimantally determined current density ~1010-1012A/m2
Tsoi et al. PRL 61, 2472 (1998)
S
F1 F2
 0.1 m
Modified Landau-Lifshitz-Gilbert
(LLG) equation

## Slide 39
In a trilayer, current direction determines the relative orientation of F1 and F2 when H = 0
Spin Transfer Torque
e-
e-
when there is a saturation field, magnetization precession radiates microwave.

## Slide 40
Landau-Lifshitz-Gilbert equation with Spin Transfer Torque terms
Current induced domain wall motion
Passing spin polarized current from Domain A to Domain BB switches
e-
e-
Berger, JAP 55, 1954 (1984)
Tatara et. al., PRL 92, 086601 (2004)
Zhang et. al., PRL 93, 127204 (2004)
Thiaville et. al., Europhys. Lett. 69, 990 (2005)
Stiles et. al., PRB 75, 214423 (2007)
Spin Transfer Torque

## Slide 41
Landau-Lifshitz-Gilbert equation with Spin Transfer Torque terms
Spin Transfer Torque
Hoop
In-plane torque
Anti-damping
Destabilizes M
Out-of-plane torque
Field-like torque
Modifies energy barrier

## Slide 42
Industrial applications
Read head in hard drives
MRAM

## Slide 43: Magnetic skyrmions
How to generate
To detect
To manipulate
Magnetic field
Electric current
Spin current, spin wave
Neel
Bloch